Synthesis and structure of tris(5-bromo-2-methoxyphenyl)antimony dicarboxylates

Artem’eva E.V.

Federal State Autonomous Educational Institution of Higher Education

“South Ural State University (NRU)”, Chelyabinsk, Russia.

katriona-art@yandex.ru

It has been found that the reactions of tris(5-bromo-2-methoxyphenyl)antimony with 2,3,4,5-tetrafluorobenzoic and pentafluoropropionic acids in the presence of tert-butyl hydroperoxide in diethyl ether at molar ratio of the reactants 1:2:1, leads to the formation of tris(5-bromo-2-methoxyphenyl)antimony dicarboxylates [(2-MeO)(5-Br)C6H3]3Sb[OC(O)R]2:

Ar3Sb + 2 HOC(O)R + t-BuOOH ® Ar3Sb(OC(O)R)2 + t-BuOH + H2O

Ar = (2-MeO)(5-Br)C6H3; R = C6F4H-6 (1), CF2CF3 (2).

The actual reaction yields are close to quantitative ones, the melting point is 224 С (1),         189 С (2).

According to X-ray diffraction analysis data, antimony atoms in molecules 1, 2 have trigonal-bipyramidal coordination with oxygen atoms of carboxyl groups in axial positions. The axial angles OSbO are equal to 177.5(2) (1), 174.4(1) (2). The angles between the axial and equatorial bonds OSbC vary in the intervals 84.0(3)–93.5(3) (1), 85.4(2)–100.2(2) (2). The sums of the valence angles CSbC in the equatorial plane for compounds 1, 2 are practically equal to 360, antimony atoms deviate from the equatorial plane by 0.043 Å (1) and 0.045 Å (2).

The mean values ​​of Sb–C bond lengths are 2.117(8) Å (1) and 2.101(5) Å (2). The Sb–O bonds are 2.108(6), 2.117(6) Å (1) and 2.113(4), 2.129(4) Å (2). Carboxylate ligands exhibit an anisobidentate binding mode; distances Sb···O=С are equal to 3.032(7), 3.200(8) Å (1) and 3.158(6), 3.171(5) Å (2). Carboxylate ligands have trans orientation towards the SbC3 fragment. The angles between carboxyl group planes are 53.13° (1) and 44.44° (2).

There are contacts Sb···OMe; distances Sb···O are 3.148(6)–3.204(7) Å (1), 3.101(4)–3.172(4) Å (2), which is much less than the sum of the van der Waals radii of antimony and oxygen atoms (3.7 Å).

Structural organization in crystals is due to С–Н··· interactions and weak hydrogen bonds C–F···H–C.